Supporting Information

Room temperature synthesis of nanometric & luminescent silver-MOFs

Vanessa Celis-Arias, Ismael A. Garduño-Wilchis, Gilberto Alarcón, Fernando González Chávez, Efrain Garrido Guerrero, Hiram I. Beltrán,* Sandra Loera-Serna*

a) b)

c)

Figure S1. a) Schematic representation of synthesis condition of Ag2BDC MOF, b) X-ray patters of molar ratio 2:1 Ag:BDC with different condition methods: SRT (stirring at room temperature), US (ultrasound assisted method) and, ST (solvothermal methodology), the red oval corresponds to Ag-NP diffraction peak and, c) XRD patter of Ag2BDC reproducibility test with STR method.

Figure S2. XRD of Ag2BDC remaining after TGA (800 ºC).

Figure S3. Structural stability (24 h) of MOF Ag2BDC up) in water, down) as synthesized.

Figure S4. Structural stability of MOFs Ag2BDC & UAM-1 in PBS, DMEM, and DMEM+FBS. Herein is clearly evidenced the formation of AgCl in all tested cases.

XRD Structural data information of UAM-1 (.cif file without structure factors).

Structure factors were not obtained since this resolution was determined by crystallographic cell enhancement, followed by ligand replacement.

#================================================================

data_Ag2NDC-UAM-1

#================================================================

_publ_section_title

;

Room temperature synthesis of nanometric & luminescent silver-MOFs

;

_publ_contact_author_name

;

Sandra Loera-Serna

Hiram Isaac Beltran

;

_publ_contact_author_address

;

Departamento de Ciencias B\'asicas, DCBI, Universidad Aut\'onoma

Metropolitana-Azcapotzalco, Av. San Pablo No 180, Col. Reynosa-Tamaulipas,

Ciudad de M\'exico. C.P. 02200, M\'exico.

;

_publ_contact_author_email

;

sls@azc.uam.mx

hibc@azc.uam.mx

;

_publ_section_abstract

;

Three silver-MOFs were prepared by an optimized, room-temperature methodology starting from AgNO₃ and dicarboxylate ligands in water/ethanol yielding Ag2BDC, Ag2NDC (UAM-1) & Ag2TDC (UAM-2) in 38-48% (BDC=benzenedicarboxylate; NDC=1,8-naphthalene-dicarboxylate; TDC=p-terphenyl-4,4′′-dicarboxylate). They were characterized by PXRD/FT-IR/TGA/photoluminescence spectroscopy, and the former two by SEM. These materials started decomposing at 330ºC evidencing stability. The crystal structure for UAM-1 was determined by PXRD, DFT calculations, and Rietveld refinement, in general, the structure is of 3D nature, where the largest Ag-O bonding is interlinking 2D-layers. FTIR spectra revealed 1450 and 1680 bands (cm-1) of asymmetric stretching aniso-/iso-bidentate -COO coordination with 2/3-Ag atoms, accompanied by Ag-O bands in 780-740, all evidenced the formation of the network. XRD and SEM, unveil nanometric-scale crystals of Ag₂BDC, and UAM-1 developed micrometric single-stranded/agglomerated fibrillar particles of varying nanometric widths. Luminescence spectroscopy presented emission of Ag₂BDC, attributed to ligand-to-metal or ligand-to-metal-metal transitions, evidencing an energy transfer due to a short distance between adjacent BDC molecules. UAM-1 and UAM-2 have not shown luminescence emission attributable to ligand-to-metal transition, presenting only emission in UV. Stability of Ag₂BDC and UAM-1 was evaluated in PBS/DMEM/DMEM+FBS media by XRD, losing their crystallinity, and yielding AgCl due to soft-soft (Pearson's principle) affinity.

;

_audit_creation_method              Expo2014

_audit_creation_date             2022-08-16

_chemical_name_systematic     Ag2NDC-UAM-1

_chemical_formula_moiety      'C12 H6 O4 Ag2'

_chemical_formula_sum         'C12 H6 O4 Ag2'

_chemical_formula_weight      429.91

_cell_formula_units_Z            2

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_source

'H'   'Hydrogen'   'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'C'   'Carbon'   'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'O'   'Oxygen'   'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Ag'   'Silver'   'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_cell_length_a                   8.3990(6)

_cell_length_b                   6.0442(3)

_cell_length_c                   5.0331(3)

_cell_angle_alpha                105.965(5)

_cell_angle_beta                 94.300(3)

_cell_angle_gamma                81.821(6)

_cell_volume                     242.98(2)

_cell_measurement_temperature    298

_exptl_crystal_description       polycrystalline

_diffrn_radiation_type          'Cu K\a~1~'

_diffrn_source                   'Cu microsource'

_diffrn_measurement_device_type

;

'Bruker Advanced D8 diffractometer, LYNXEYE detector'

;

_computing_cell_refinement       'EXPO 2014 (Altomare 2014)'

_computing_structure_solution    'EXPO 2014 (Altomare 2014)'

_computing_structure_refinement  'EXPO 2014 (Altomare 2014)'

_diffrn_ambient_temperature     298

_diffrn_radiation_wavelength     1.540560

_symmetry_Int_Tables_number         2

_symmetry_cell_setting              triclinic

_symmetry_space_group_name_H-M      'P -1'

_symmetry_space_group_name_hall     '-P 1'

loop_

_symmetry_equiv_pos_site_id

_symmetry_equiv_pos_as_xyz

1   'x, y, z'

2   '-x, -y, -z'

loop_

_pd_proc_ls_profile_function     pseudo-Voigt

_pd_proc_ls_background_function

;

Background modelled by a Chebyshev polynomial of degree 19

b1        3102(3)

b2        -691(3)

b3        29(3)

b4        127(3)

b5        -75(2)

b6        94(2)

b7        -1(3)

b8        -24(3)

b9        28(2)

b10       -14(2)

b11       31(2)

b12       -21(2)

b13       -8(2)

b14       -4(2)

b15       5(2)

b16       3(2)

b17       43(2)

b18       6.1(19)

b19       4.6(19)

zero      0.2218(5)

sample di.0.007538527

sample tr.-0.0001194932

scale     0.000901(7)

;

_pd_calc_method                  'Rietveld Refinement'

#---- raw/calc data loop -----

_pd_meas_2theta_range_min        6.0000

_pd_meas_2theta_range_max        70.0000

_pd_meas_2theta_range_inc        0.0197

_pd_proc_2theta_range_min        6.0000

_pd_proc_2theta_range_max        70.0000

_pd_proc_2theta_range_inc        0.0197

_pd_meas_number_of_points        3255

_pd_proc_number_of_points        3255

_pd_proc_ls_prof_R_factor        0.02429

_pd_proc_ls_prof_wR_factor        0.03292

_pd_proc_ls_prof_wR_expected       0.02199

_refine_ls_R_Fsqd_factor          0.06622

_reflns_number_total             210

_reflns_limit_h_max              6

_reflns_limit_k_max              4

_reflns_limit_l_max              3

_reflns_d_resolution_high        1.34294

# ATOMIC COORDINATES AND DISPLACEMENT PARAMETERS

loop_

_atom_site_type_symbol

_atom_site_label

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_occupancy

_atom_site_adp_type

C        C1        0.8779 1.2630 0.9249 0.0127 1.0000        Uiso

C        C2        0.8779 1.2630 0.9249 0.0127 1.0000        Uiso

C        C3        0.7783 1.1625 0.7069 0.0127 1.0000        Uiso

C        C4        0.7783 1.1625 0.7069 0.0127 1.0000        Uiso

H        H1        0.6914 1.2711 0.6098 0.0152 1.0000        Uiso

H        H2        0.6914 1.2711 0.6098 0.0152 1.0000        Uiso

C        C5        -0.0064 0.1240 0.0509 0.0127 1.0000        Uiso

C        C6        -0.0064 0.1240 0.0509 0.0127 1.0000        Uiso

C        C7        0.9000 0.7783 0.7317 0.0127 1.0000        Uiso

C        C8        0.1000 0.2217 0.2683 0.0127 1.0000        Uiso

H        H3        0.9052 0.5901 0.6570 0.0152 1.0000        Uiso

H        H4        0.0948 0.4099 0.3430 0.0152 1.0000        Uiso

C        C9        0.7869 0.9170 0.6136 0.0127 1.0000        Uiso

C        C10       0.2131 0.0830 0.3864 0.0127 1.0000        Uiso

C        C11       0.6729 0.7997 0.3960 0.0127 1.0000        Uiso

C        C12       0.3271 0.2003 0.6040 0.0127 1.0000        Uiso

O        O1        0.6127 0.8984 0.2110 0.0127 1.0000        Uiso

O        O2        0.3873 0.1016 0.7890 0.0127 1.0000        Uiso

O        O3        0.6452 0.6012 0.4137 0.0127 1.0000        Uiso

O        O4        0.3548 0.3988 0.5863 0.0127 1.0000        Uiso

H        H5        0.8674 1.4514 1.0037 0.0152 1.0000        Uiso

H        H6        0.8674 1.4514 1.0037 0.0152 1.0000        Uiso

Ag       Ag1       0.5337 0.3115 0.1316 0.0127 1.0000        Uiso

Ag       Ag2       0.4663 0.6885 0.8684 0.0127 1.0000        Uiso

# MOLECULAR GEOMETRY

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

C1 C4  1.382933 .

C1 C6  1.421720 1_666

C1 H6  1.090919 .

C2 C3  1.382933 .

C2 C5  1.421722 1_666

C2 H5  1.090929 .

C3 H2  1.090781 .

C3 C10  1.420519 2_666

C4 H1  1.090792 .

C4 C9  1.420505 .

C5 C2  1.421722 1_444

C5 C6  1.435133 2_555

C5 C7  1.412118 2_666

C6 C1  1.421727 1_444

C6 C5  1.435133 2_555

C6 C8  1.412116 .

C7 C5  1.412117 2_666

C7 H4  1.090545 2_666

C7 C10  1.386132 2_666

C8 H3  1.090534 2_666

C8 C9  1.386139 2_666

H3 C8  1.090537 2_666

H4 C7  1.090548 2_666

C9 C8  1.386140 2_666

C9 C12  1.492947 2_666

C10 C4  1.420511 2_666

C10 C7  1.386130 2_666

C10 C11  1.492939 2_666

C11 C10  1.492936 2_666

C11 O2  1.275257 2_666

C11 O4  1.281428 2_666

C12 C9  1.492943 2_666

C12 O1  1.275276 2_666

C12 O3  1.281407 2_666

O1 C12  1.275274 2_666

O1 Ag1  2.240486 2_665

O1 Ag2  2.621906 2_676

O2 C11  1.275256 2_666

O2 Ag1  2.240485 1_556

O2 Ag2  2.621915 1_545

O3 C12  1.281406 2_666

O3 Ag1  2.720552 2_666

O3 Ag2  2.204131 2_666

O4 C11  1.281427 2_666

O4 Ag1  2.204118 2_666

O4 Ag2  2.720536 2_666

Ag1 O1  2.621920 1_545

Ag1 O1  2.240485 2_665

Ag1 O3  2.720548 2_666

Ag1 O4  2.204117 2_666

Ag2 O1  2.621908 2_676

Ag2 O2  2.240478 2_667

Ag2 O3  2.204129 2_666

Ag2 O4  2.720532 2_666

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

C4 C1 H6   120.00 . .

C1 C4 H1   120.17 . .

C1 C4 C9   119.82 . .

C3 C2 H5   120.00 . .

C2 C3 H2   120.17 . .

H1 C4 C9   120.00 . .

C4 C9 C7   120.16 . .

C4 C9 C11   122.05 . .

C6 C8 H4   119.58 . .

C6 C8 C10   121.24 . .

H3 C7 C9   119.18 . .

C7 C9 C11   117.75 . .

H4 C8 C10   119.18 . .

C8 C10 C12   117.75 . .

C9 C11 O1   119.58 . .

C9 C11 O3   114.91 . .

C10 C12 O2   119.58 . .

C10 C12 O4   114.91 . .

O1 C11 O3   125.50 . .

C11 O3 Ag1   134.09 . .

C11 O3 Ag2   105.84 . .

O2 C12 O4   125.50 . .

C12 O4 Ag1   105.84 . .

C12 O4 Ag2   134.09 . .

Ag1 O3 Ag2   101.07 . .

O3 Ag1 O4    78.93 . .

O3 Ag2 O4    78.93 . .

Ag1 O4 Ag2   101.07 . .

loop_

_geom_torsion_atom_site_label_1

_geom_torsion_atom_site_label_2

_geom_torsion_atom_site_label_3

_geom_torsion_atom_site_label_4

_geom_torsion

_geom_torsion_site_symmetry_1

_geom_torsion_site_symmetry_2

_geom_torsion_site_symmetry_3

_geom_torsion_site_symmetry_4

C6 C1 C4 H1  -178.99 1_666 . . .

C6 C1 C4 C9     2.41 1_666 . . .

H6 C1 C4 H1     1.63 . . . .

H6 C1 C4 C9  -176.98 . . . .

C5 C2 C3 H2  -178.99 1_666 . . .

C5 C2 C3 C10     2.41 1_666 . . 2_666

H5 C2 C3 H2     1.63 . . . .

H5 C2 C3 C10  -176.98 . . . 2_666

C2 C3 C10 C7    -3.06 . . 2_666 .

C2 C3 C10 C11   174.60 . . 2_666 .

H2 C3 C10 C7   178.34 . . 2_666 .

H2 C3 C10 C11    -4.01 . . 2_666 .

C1 C4 C9 C8    -3.05 . . . 2_666

C1 C4 C9 C12   174.60 . . . 2_666

H1 C4 C9 C8   178.34 . . . 2_666

H1 C4 C9 C12    -4.01 . . . 2_666

C2 C5 C7 H4    -0.32 1_444 . 2_666 .

C2 C5 C7 C10  -179.31 1_444 . 2_666 .

C6 C5 C7 H4   177.77 2_555 . 2_666 .

C6 C5 C7 C10    -1.23 2_555 . 2_666 .

C1 C6 C8 H3    -0.32 1_444 . . 2_666

C1 C6 C8 C9  -179.31 1_444 . . 2_666

C5 C6 C8 H3   177.77 2_555 . . 2_666

C5 C6 C8 C9    -1.23 2_555 . . 2_666

C5 C7 C10 C3     1.22 2_666 . 2_666 .

C5 C7 C10 C11  -176.54 2_666 . 2_666 .

H4 C7 C10 C3  -179.79 2_666 . 2_666 .

H4 C7 C10 C11     2.46 2_666 . 2_666 .

C6 C8 C9 C12   176.54 . . 2_666 .

H3 C8 C9 C12    -2.46 2_666 . 2_666 .

C4 C9 C8 H3  -179.79 . . 2_666 .

C12 C9 C8 H3     2.46 2_666 . 2_666 .

C4 C9 C12 O1    29.58 . . 2_666 .

C4 C9 C12 O3  -150.96 . . 2_666 .

C8 C9 C12 O1  -152.72 2_666 . 2_666 .

C8 C9 C12 O3    26.74 2_666 . 2_666 .

C4 C10 C7 C5    -1.22 2_666 . 2_666 .

C4 C10 C7 H4   179.79 2_666 . 2_666 .

C11 C10 C7 C5   176.54 2_666 . 2_666 .

C11 C10 C7 H4    -2.46 2_666 . 2_666 .

C4 C10 C11 O2   -29.58 2_666 . 2_666 .

C4 C10 C11 O4   150.96 2_666 . 2_666 .

C7 C10 C11 O2   152.72 2_666 . 2_666 .

C7 C10 C11 O4   -26.74 2_666 . 2_666 .

O2 C11 C10 C3    29.58 2_666 . 2_666 .

O2 C11 C10 C7  -152.72 2_666 . 2_666 .

O4 C11 C10 C3  -150.96 2_666 . 2_666 .

O4 C11 C10 C7    26.74 2_666 . 2_666 .

C10 C11 O4 Ag1  -165.91 2_666 . 2_666 .

C10 C11 O4 Ag2    70.53 2_666 . 2_666 .

O2 C11 O4 Ag1    13.52 2_666 . 2_666 .

O2 C11 O4 Ag2  -110.05 2_666 . 2_666 .

O1 C12 C9 C8   152.72 2_666 . 2_666 .

O3 C12 C9 C8   -26.74 2_666 . 2_666 .

C9 C12 O3 Ag1   -70.53 2_666 . 2_666 .

C9 C12 O3 Ag2   165.91 2_666 . 2_666 .

O1 C12 O3 Ag1   110.05 2_666 . 2_666 .

O1 C12 O3 Ag2   -13.51 2_666 . 2_666 .

Ag1 O1 C12 C9   173.15 2_665 . 2_666 .

Ag1 O1 C12 O3    -6.25 2_665 . 2_666 .

Ag2 O1 C12 C9   -28.05 2_676 . 2_666 .

Ag2 O1 C12 O3   152.56 2_676 . 2_666 .

Ag1 O2 C11 C10  -173.15 1_556 . 2_666 .

Ag1 O2 C11 O4     6.25 1_556 . 2_666 .

Ag2 O2 C11 C10    28.05 1_545 . 2_666 .

Ag2 O2 C11 O4  -152.56 1_545 . 2_666 .

Ag1 O3 C12 C9    70.53 2_666 . 2_666 .

Ag1 O3 C12 O1  -110.05 2_666 . 2_666 .

Ag2 O3 C12 C9  -165.91 2_666 . 2_666 .

Ag2 O3 C12 O1    13.51 2_666 . 2_666 .

C12 O3 Ag1 O4   142.42 2_666 . 2_666 .

Ag2 O3 Ag1 O4    -0.02 2_666 . 2_666 .

C12 O3 Ag2 O4  -125.23 2_666 . 2_666 .

Ag1 O3 Ag2 O4     0.02 2_666 . 2_666 .

Ag1 O4 C11 C10   165.91 2_666 . 2_666 .

Ag1 O4 C11 O2   -13.52 2_666 . 2_666 .

Ag2 O4 C11 C10   -70.53 2_666 . 2_666 .

Ag2 O4 C11 O2   110.04 2_666 . 2_666 .

C11 O4 Ag1 O3   125.23 2_666 . 2_666 .

Ag2 O4 Ag1 O3     0.00 2_666 . 2_666 .

C11 O4 Ag2 O3  -142.42 2_666 . 2_666 .

Ag1 O4 Ag2 O3     0.00 2_666 . 2_666 .

O1 Ag1 O3 C12   -23.11 1_545 . 2_666 .

O1 Ag1 O3 Ag2   119.31 1_545 . 2_666 .

O1 Ag1 O3 C12    54.79 2_665 . 2_666 .

O1 Ag1 O3 Ag2  -162.78 2_665 . 2_666 .

O4 Ag1 O3 C12  -142.42 2_666 . 2_666 .

O4 Ag1 O3 Ag2     0.02 2_666 . 2_666 .

O1 Ag1 O4 C11   156.50 1_545 . 2_666 .

O1 Ag1 O4 Ag2   -78.27 1_545 . 2_666 .

O1 Ag1 O4 C11   -21.99 2_665 . 2_666 .

O1 Ag1 O4 Ag2   103.23 2_665 . 2_666 .

O3 Ag1 O4 C11  -125.23 2_666 . 2_666 .

O3 Ag1 O4 Ag2     0.00 2_666 . 2_666 .

O1 Ag2 O3 C12  -156.50 2_676 . 2_666 .

O1 Ag2 O3 Ag1    78.27 2_676 . 2_666 .

O2 Ag2 O3 C12    21.99 2_667 . 2_666 .

O2 Ag2 O3 Ag1  -103.23 2_667 . 2_666 .

O4 Ag2 O3 C12   125.23 2_666 . 2_666 .

O4 Ag2 O3 Ag1    -0.03 2_666 . 2_666 .

O1 Ag2 O4 C11    23.11 2_676 . 2_666 .

O1 Ag2 O4 Ag1  -119.31 2_676 . 2_666 .

O2 Ag2 O4 C11   -54.79 2_667 . 2_666 .

O2 Ag2 O4 Ag1   162.78 2_667 . 2_666 .

O3 Ag2 O4 C11   142.42 2_666 . 2_666 .

O3 Ag2 O4 Ag1     0.00 2_666 . 2_666 .