Supplementary Data

The modulus of elasticity (E-modulus) was calculated as follows:

(1)

L (the fulcrum span) = 18 mm, F was a deflection, and I was a moment of inertia of fracture surface caused by the three-point bending mechanical test.

The energy to failure was calculated as follows:

(2)

Work-of-fracture for the three-point bending test was calculated as the area under the load-displacement curve divided by the specimen's cross-sectional area, and reported in units of J/m2. F was a deflection.

(3)

aout (long half axes of the outer ring of collected femur) = 2.25 mm, bout (short half axes of the outer ring of collected femur) = 1.75 mm, the long and short half axes of the inner ring were ain (long half axes of the inner ring of the collected femur) = 1.5 mm, bin (short half axes of the inner ring of collected femur) = 1 mm, A was the cross-sectional area of the fracture, and F was a deflection.

Fig. S1 Surgical procedures of right femoral DO in the rat.